**Colorado Rose Red Granite**

Specification sheet

SPG 2.655

Absorption .20

Solid Weight 175 lb/cuft

Corroded Weight 89 lb/cuft

LA Abrasion 27%

Crushing Strength 28,000 psi

Colorado Rose Red Inc. 148 Cheyenne Ct Lyons CO 80540 P: 3037473718 F:3033626353